## Slide 1: SOME STUDY RESULTS OF COLOR CHANGES DEPENDING ON MONGOLIAN ENVIRONMENTAL CONDITION
Otgonsuvd Badrakh,
Batzaya.E, Galbaatar.T, Oyuntulga.M
ISGC 2021
Institute of Mathematics and Digital technology
Mongolian Academy of Sciences

## Slide 2: Contents
Color measurement
Materials and methods
Results and discussion
Conclusion
References

## Slide 3: Color measurements
Visual color measurement Instrumental color measurements

## Slide 4: Color spaces
CIE 1931- XYZ
CIE 1976- L*a*b*
Munsell 1913- L*H*C*

## Slide 5: Research materials and methods

## Slide 6: Measurement
№ | Colorants | Origin
1 | Red pigment | Korea
2 | Green pigment | Korea
3 | Blue pigment | Korea
4 | Yellow pigment | Korea
5 | Red dye | Russia
6 | Green dye | Russia
7 | Blue dye | Russia
8 | Yellow dye | Russia
9 | White dye | Russia
Measurement device: X-rite i1 Pro Colorimeter
Measurement sample

## Slide 7: Research method
Color measurement
Create a database
Processing of measurement results
Analyze the data

## Slide 8: Method of color measurement
Object
Prepare the measurement object
Device
Prepare the instrument by dialing and selecting the measurement mode
Measurement Settings
Make measurement callibration
Reflectance calibration
Save data
Read color
Make a white tile callibration
Make color measurements

## Slide 9: Method of Data processing
Mean
Variance
Standard deviation
Coefficient of Skewness
Coefficient of Kurtosis
Regression

## Slide 10: Results and discussion

## Slide 11: Shortterm measurements result
 | XYZ_X | XYZ_Y | XYZ_Z | LAB_L | LAB_A | LAB_B | LAB_C | LAB_H
1 | 20.50452 | 11.3803 | 1.778595 | 40.214 | 56.14 | 41.263 | 69.673 | 36.3
2 | 18.65532 | 10.35196 | 1.69615 | 38.467 | 54.414 | 39.124 | 67.02 | 35.7
3 | 19.69677 | 10.95863 | 1.843279 | 39.511 | 55.199 | 39.384 | 67.809 | 35.5
4 | 20.59455 | 11.44771 | 1.831663 | 40.325 | 56.099 | 40.906 | 69.429 | 36.1
5 | 18.7982 | 10.65397 | 1.935784 | 38.991 | 52.889 | 37.562 | 64.87 | 35.4
2020.02.05 : red pigment

## Slide 12: Longterm measurements result
 | Red pigment | XYZ_X | XYZ_Y | XYZ_Z | LAB_L | LAB_A | LAB_B
1 | 2020.02.05 | 18.85279 | 10.29676 | 1.560897 | 38.37 | 55.849 | 40.454
2 | 2020.02.14 | 18.23383 | 9.872264 | 1.516018 | 37.612 | 55.904 | 39.663
3 | 2020.02.27 | 15.44793 | 8.36504 | 1.623151 | 34.732 | 52.888 | 33.482
4 | 2020.03.06 | 15.45708 | 8.389712 | 1.75066 | 34.782 | 52.727 | 32.19
5 | 2020.03.13 | 14.46958 | 7.947754 | 1.854267 | 33.874 | 50.728 | 29.553
6 | 2020.03.20 | 14.46514 | 8.078214 | 2.014673 | 34.145 | 49.531 | 28.439
7 | 2020.03.27 | 13.94034 | 7.936497 | 2.163865 | 33.85 | 47.55 | 26.532
8 | 2020.04.10 | 13.47603 | 7.732853 | 2.131381 | 33.42 | 46.457 | 26.089
9 | 2020.04.17 | 13.48539 | 7.910743 | 2.376161 | 33.796 | 44.896 | 24.556
10 | 2020.04.23 | 12.60324 | 7.512796 | 2.406031 | 32.947 | 42.77 | 22.836
11 | 2020.05.01 | 13.04609 | 7.700111 | 2.340566 | 33.35 | 43.969 | 24.095
12 | 2020.05.06 | 13.59228 | 8.026753 | 2.424199 | 34.039 | 44.536 | 24.563
13 | 2020.05.18 | 13.13937 | 7.833495 | 2.475053 | 33.634 | 43.358 | 23.437
14 | 2020.05.22 | 12.77753 | 7.607822 | 2.339225 | 33.152 | 43.048 | 23.765

## Slide 13: Statistical analysis of shortterm measurements
Statistical parameter | LAB_L | LAB_A | LAB_B | LAB_C | LAB_H
Mean | 39.5016 | 54.9482 | 39.6478 | 67.7602 | 35.8
Standard Error | 0.354732 | 0.605529 | 0.666575 | 0.875992 | 0.173205
Median | 39.511 | 55.199 | 39.384 | 67.809 | 35.7
Standard Deviation | 0.793205 | 1.354004 | 1.490508 | 1.958777 | 0.387298
Sample Variance | 0.629175 | 1.833326 | 2.221614 | 3.836808 | 0.15
Kurtosis | -1.90266 | 0.121249 | -0.82762 | -0.25435 | -2.2
Skewness | -0.26779 | -0.94861 | -0.38137 | -0.71531 | 0.430331
Range | 1.858 | 3.251 | 3.701 | 4.803 | 0.9
Minimum | 38.467 | 52.889 | 37.562 | 64.87 | 35.4
Maximum | 40.325 | 56.14 | 41.263 | 69.673 | 36.3
Sum | 197.508 | 274.741 | 198.239 | 338.801 | 179
Count | 5 | 5 | 5 | 5 | 5

## Slide 14: Statistical analysis of longterm measurements
Statistical parameter | LAB_L | LAB_A | LAB_B
Mean | 34.40736 | 48.15793 | 28.54671
Standard Error | 0.430888 | 1.270207 | 1.567719
Median | 33.862 | 47.0035 | 26.3105
Standard Deviation | 1.612235 | 4.752681 | 5.865868
Sample Variance | 2.599303 | 22.58797 | 34.4084
Kurtosis | 2.715926 | -1.26491 | 0.227765
Skewness | 1.860959 | 0.484197 | 1.140272
Range | 5.423 | 13.134 | 17.618
Minimum | 32.947 | 42.77 | 22.836
Maximum | 38.37 | 55.904 | 40.454
Sum | 481.703 | 674.211 | 399.654
Count | 14 | 14 | 14

## Slide 15: Data analysis 1:
Chart: Red pigment
LAB_L | 38.37 | 37.612 | 34.732 | 34.782 | 33.874 | 34.145 | 33.85 | 33.42 | 33.796 | 32.947 | 33.35 | 34.039 | 33.634 | 33.152
LAB_A | 55.849 | 55.904 | 52.888 | 52.727 | 50.728 | 49.531 | 47.55 | 46.457 | 44.896 | 42.77 | 43.969 | 44.536 | 43.358 | 43.048
LAB_B | 40.454 | 39.663 | 33.482 | 32.19 | 29.553 | 28.439 | 26.532 | 26.089 | 24.556 | 22.836 | 24.095 | 24.563 | 23.437 | 23.765

## Slide 16: Data analysis 2:
Chart: Green pigment
LAB_L | 42.541 | 41.82 | 41.197 | 41.459 | 41.452 | 40.895 | 41.839 | 42.143 | 41.458 | 34.138 | 39.113 | 35.764 | 40.707 | 40.611
LAB_A | -16.023 | -16.517 | -15.936 | -16.193 | -15.618 | -15.294 | -15.557 | -14.797 | -15.349 | -12.118 | -14.018 | -13.144 | -14.626 | -15.007
LAB_B | 14.209 | 14.054 | 13.612 | 13.784 | 14.027 | 13.755 | 14.323 | 14.551 | 13.734 | 12.942 | 12.76 | 11.799 | 13.487 | 13.355

## Slide 17: Data analysis 3:
Chart: Blue pigment
LAB_L | 29.975 | 30.116 | 29.198 | 29.507 | 28.875 | 28.828 | 28.95 | 28.721 | 29.021 | 28.689 | 28.801 | 28.263 | 28.729 | 29.036
LAB_A | 26.364 | 23.863 | 24.413 | 24.597 | 25.17 | 25.153 | 25.038 | 25.239 | 25.307 | 24.516 | 25.22 | 24.135 | 24.685 | 24.1
LAB_B | -68.743 | -66.891 | -66.411 | -66.942 | -66.682 | -66.387 | -66.326 | -66.363 | -66.214 | -64.983 | -65.694 | -64.097 | -64.812 | -64.858

## Slide 18: Data analysis 4:
Chart: Yellow pigment
LAB_L | 76.785 | 75.53 | 73.963 | 69.872 | 73.194 | 72.868 | 72.586 | 72.618 | 73.009 | 71.689 | 71.525 | 71.957 | 72.207 | 71.741
LAB_A | 28.298 | 23.362 | 22.309 | 20.222 | 22.137 | 21.578 | 21.436 | 22.686 | 20.797 | 21.573 | 21.758 | 20.649 | 21.205 | 20.64
LAB_B | 81.57 | 78.738 | 75.762 | 72.117 | 73.777 | 72.829 | 72.178 | 72.396 | 72.844 | 71.394 | 70.559 | 71.376 | 71.953 | 72.399

## Slide 19: Data analysis 6:
Chart: Green dye
LAB_L | 45.734 | 44.737 | 44.803 | 45.085 | 44.843 | 44.938 | 45.301 | 42.295 | 45.405 | 45.486 | 45.331 | 45.287 | 45.347 | 45.452
LAB_A | -42.997 | -41.997 | -41.563 | -41.729 | -41.073 | -40.775 | -40.755 | -38.786 | -40.377 | -40.615 | -40.236 | -40.228 | -40.321 | -40.071
LAB_B | 7.691 | 7.269 | 6.674 | 6.502 | 6.182 | 5.808 | 5.491 | 4.989 | 4.353 | 4.494 | 4.366 | 4.13 | 3.96 | 3.923

## Slide 20: Data analysis 7:
Chart: Blue dye
LAB_L | 61.927 | 61.082 | 61.151 | 51.157 | 61.325 | 61.133 | 61.345 | 61.511 | 61.405 | 61.304 | 61.171 | 61.201 | 61.277 | 61.256
LAB_A | -23.253 | -22.576 | -22.641 | -20.113 | -23.063 | -22.968 | -23.132 | -23.612 | -23.157 | -23.345 | -23.369 | -23.176 | -23.211 | -23.314
LAB_B | -36.044 | -35.489 | -35.31 | -32.361 | -35.011 | -34.637 | -34.324 | -33.805 | -34.406 | -33.888 | -33.324 | -33.753 | -33.486 | -33.367

## Slide 21: Data analysis 8:
Chart: Yellow dye
LAB_L | 81.844 | 80.706 | 80.607 | 80.589 | 80.549 | 64.759 | 79.623 | 80.409 | 80.53 | 80.263 | 80.161 | 80.149 | 80.171 | 80.157
LAB_A | 13.856 | 13.689 | 13.775 | 13.898 | 13.898 | 11.348 | 13.936 | 14.46 | 13.806 | 14.077 | 14.065 | 13.908 | 13.861 | 13.953
LAB_B | 69.649 | 69.053 | 68.633 | 68.403 | 67.893 | 55.808 | 66.418 | 66.44 | 66.106 | 65.645 | 65.213 | 64.499 | 64.671 | 64.64

## Slide 22: Data analysis 9:
Chart: White dye
LAB_L | 92.423 | 90.849 | 90.711 | 90.755 | 90.619 | 90.365 | 89.845 | 90.386 | 89.469 | 90.339 | 90.012 | 90.028 | 90.031 | 89.88
LAB_A | 0.245 | 0.527 | 0.56 | 0.621 | 0.568 | 0.929 | 1.024 | 1.32 | 1.201 | 1.283 | 1.331 | 1.407 | 1.45 | 1.457
LAB_B | 4.209 | 4.945 | 4.913 | 5.136 | 4.981 | 5.819 | 5.819 | 6.368 | 6.927 | 6.473 | 6.5 | 6.572 | 6.698 | 6.781

## Slide 23: Results
№ | Colorants | L*-R2 | a*- R2 | b*- R2
 | Red pigment | 0.9195 | 0.5836 | 0.8209
 | Green pigment | 0.2639 | 0.3474 | 0.4832
 | Blue pigment | 0.5645 | 0.0899 | 0.7821
 | Yellow pigment | 0.5772 | 0.3667 | 0.3812
 | Red dye | 0.4968 | 0.0422 | 0.7847
 | Green dye | 0.0141 | 0.5819 | 0.958
 | Blue dye | 0.0479 | 0.1661 | 0.4255
 | Yellow dye | 0.0007 | 0.0338 | 0.1722
 | White dye | 0.5535 | 0.9182 | 0.8614

## Slide 24: Conclusion
In the future, it is necessary to increase the measurement data and perform more detailed data analysis, and we are aiming to determine the initial color of the object using machine learning methods based on regression analysis using the color measurement values. Further research is needed to improve the number and quality of measurement objects.

## Slide 25: Future research

## Slide 26: References
Roy S. Berns, “Principles of Color Technology”, New York, John Wiley& Sons, 2000
Kurt Nassau, “Color for Science, Art and Technology”, Netherland, Elsevier, 2006
User Manual of X-rite i1 Pro Colorimeter, China, Trademark of X-rite, 2017
Ganesh Ramanathan, Understanding Tristimulus Values: Taking the Guesswork Out of Color Measurement Instrumentation, hunterlab.com, 2015
Ч.Авдай, Д.Энхтуяа,”Судалгаа шинжилгээний ажил гүйцэтгэх арга зүй”, Улаанбаатар, 2015
F.M. Dekking C. Kraaikamp, H.P. Lopuhaa¨ L.E. Meester, “A Modern Introduction to Probability and Statistics”, ISBN 978-1-85233-896-1, Springer, 2013
Siegmund Brandt, Data Analysis Statistical and Computational Methods for Scientists and Engineers, ISBN 978-3-319-03761-5 , DOI 10.1007/978-3-319-03762-2, Springer, 2014
Maria Elena Radulescu-Grad, Gabriela Vlase , Gheorghe Ilia, Adelina Andelescu, “Simona Popa, Amido Black 10B Dye Copper Complex–Synthesis, Characterization and Color Analysis”, Revista de Chimie 71 (8), https://doi.org/10.37358/RC.20.8.8276, 2020, 27-38
J Suwanboriboon, W Meesiri, W Wongkokua, “An application of spectrophotometer for ADMI color measurement”, Journal of Physics:1144, doi :10.1088/1742-6596/1144/1/012064, 2018

## Slide 27: Thank you for the attention 